INTISARI

Penelitian ini berjudul Uji Perubahan Karakteristik Tepung Umbi Bit (Beta vulgaris L.) yang Dikemas Selama Penyimpanan. Tujuan penelitian adalah  untuk menguji perubahan karakteristik terhadap tepung umbi bit (Beta vulgaris L.) yang dikemas dengan berbagai jenis kemasan plastik PP, LDPE dan HDPE selama penyimpanan dalam rangka meningkatkan daya simpan dan daya tarik (penerimaan konsumen).

Rancangan percobaan yang digunakan dalam penelitian ini adalah analisis regresi linear sederhana. Rancangan perlakuan ini terdiri dari 3 (tiga) kali ulangan dan 2 (dua) variabel, yaitu hubungan yang meliputi lama penyimpanan terhadap parameter yang digunakan, maka variabel bebas X = lama penyimpanan yang disimpan selama 1 bulan kemudian diamati setiap minggu dan variabel tak bebas Y = nilai respon yang diukur yaitu kadar air (gravimetri) dan kadar pati (luff’s schoorl) yang dikemas pada jenis kemasan PP, LDPE dan HDPE, untuk sampel yang terbaik dilakukan analisis kimia berupa aktivitas antioksidan (DPPH).

Dari hasil analisis regresi linear sederhana didapat sampel yang terbaik yaitu tepung umbi bit yang dikemas menggunakan kemasan plastik HDPE, selama penyimpanan 1 bulan dengan kadar air 7,8%, kadar pati 62,670% dan uji aktivitas antioksidan tepung umbi bit memiliki intensitas kuat karena nilai IC50 adalah 85,78212 ppm.

ABSTRACT

The research was The Tested Changes of Characteristics Beet Tuber (Beta vulgaris L.) Flour Packed During Storage. The research objective was to examine changes in the characteristics of the tuber flour beet (Beta vulgaris L.) which is packed with various types of plastic packaging PP, LDPE and HDPE for storage in order to increase the shelf life and appeal (consumer acceptance).

The experimental design used in this study was a simple linear regression analysis. The design of this treatment consists of 3 (three) replications and 2 (two) variables, the independent variable X = storage time stored for 1 month and then observed every week and dependent variable Y = response value measured the water content (gravimetric) & starch content (luff's schoorl) are packaged in packaging types PP, LDPE and HDPE, to the best sample performed chemical analysis in the form of antioxidant activity (DPPH).

The best sample from the results of simple linear regression analysis was beet tuber flour was packed using HDPE plastic containers for storage of one month with a water content of 7.8%, 62.670% starch content and antioxidant activity test  bit tuber flour has a stronger intensity as the IC50 value is 85.78212 ppm.